泉州车宝汽车用品有限公司

Quanzhou Chebao Automobile Accessories Co., Ltd.

报告编号/Report No.：{报告编号}

制动液型式检验报告

Brake Fluid Type Inspection Report

机动车辆制动液型式检验 Type Testing of Brake Fluids

项目名称:

Project Name:

泉州车宝汽车用品有限公司 Quanzhou Chebao Automobile Accessories Co., Ltd.

检验单位:

Inspection Company:

常规型式检验 Routine Type Inspection

检验类别:

Inspection Category:

{检验日期}

检验日期:

Report Date:

第1页 共7页

Page 1 of 7

检验时间/Test Date ：{检验日期} 检验地点/Testing Lab ：福建省泉州市鲤城区江南高新电子技术园紫安路5号 (No. 5 Zi'an Road, Jiangnan High-tech Electronic Technology Park, Licheng District, Quanzhou City, Fujian Province) 检验类别/Category Of Inspection: A:发货检验/Outgoing Inspection B:常规型式检验/Routine Type Inspection C:样品测试检验/ 生产单位/Manufacturer:泉州车宝汽车用品有限公司/Quanzhou Chebao Automobile Accessories Co., Ltd. 规格型号/Model: {规格型号} 订单号/Order No.: {订单号} 商标/Trademark: {商标} 包装规格/Packaging Size: {包装规格} Main Equipment for inspection/检验用主要仪器设备 序号; Equipment Name/设备名称; Model/型号. 1; Low temperature kinematic viscosity tester 低温运动粘度测定仪; BF-03B. 2; Petroleum product kinematic viscosity tester石油产品运动粘度测定仪; BF-03. 3; Ebulliometer/ 沸点测定仪; BF-53. 4; PH meter/PH计; PHS-25. 5; Stopwatch/秒表; XL-011. 6; Caliper/游标卡尺; c01319. 7; Analytical balance/分析天平; JJ224BC. 8; Measuring microscope/测量显微镜; 15J. 9; Shore hardness tester/邵尔硬度计; LX-A. 10; Aneroid barometer/空盒气压表; DYM3. 11; High temperature machine/高温试验箱; ED115. 12; BF high-temperature stability tester/制动液高温稳定性测定仪; BF-53. Note: All testing equipment is within the calibration validity period 注：检测设备均在计量检定/校准有效期内. 结论：经检验，被检验样品的所检项目质量指标符合GB 12981-2012《机动车辆制动液》中 {制动液名称} 机动车辆制动液的相应要求。具体检验数据及结果详见报告第2页 Conclusion: After inspection, the quality indicators of the tested items for the sample comply with the corresponding requirements for {制动液名称} motor vehicle brake fluids as specified in GB 12981-2012 <Motor vehicle brake fluids>. For detailed inspection data and results, please refer to page 2 of this report..

第2页 7页

Page 2 of 7

制动液型式检验报告

Brake Fluid Type Inspection Report

报告编号/Report No.：{报告编号}

| 制动液名称/Brake Fluid Name |  |  |  |  |  |  |  | {制动液名称} |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 批号/Batch No. |  |  |  |  |  |  |  | {检验批次} |  |  |  |
| 检测日期/Test Date |  |  |  |  |  |  |  | {检验日期} |  |  |  |
| 执行标准/Executive Standard |  |  |  |  |  |  |  | GB 12981-2012《机动车制动液》<Motor vehicle brake fluids> |  |  |  |
| 序号 NO. | 检验项目 Test Items |  |  |  | 单位 Unit | 质量指标/Quality Indicators |  |  |  |  | 检验结果 Test Results |
|  |  |  |  |  |  | {制动液名称} HZY4 HZY5 HZY7 |  |  |  |  |  |
| 1 | 外观/Appearance |  |  |  | ------ | 清亮透明，无悬浮物，杂质及沉淀 Clear and transparent, free from suspended matter, impurities, and sediment. |  |  |  |  | 清亮透明，无悬浮物，杂质及沉淀 Clear and transparent, free from suspended matter, impurities, and sediment. |
| 2 | 平衡回流沸点/Equilibrium Reflux Boiling Point |  |  |  | ℃ | {平衡回流沸点标准值} |  |  |  |  | {平衡回流沸点} |
| 3 | 湿平衡回流沸点/Wet Equilibrium Reflux Boiling Point |  |  |  | ℃ | {湿平衡回流沸点标准值} |  |  |  |  | {湿平衡回流沸点} |
| 4 | 电导率/Conductivity |  |  |  | μS/cm | 实测/Test Results |  |  |  |  | {电导率} |
| 5 | 运动粘度/Viscosity |  | -40℃ |  | mm²/s | {-40运动粘度标准值} |  |  |  |  | {运动粘度-40} |
|  |  |  | 100℃ |  | mm²/s | {100运动粘度标准值} |  |  |  |  | {运动粘度100} |
| 6 | pH值/pH |  |  |  | ------ | 7.0 ～ 11.5 |  |  |  |  | {pH} |
|  | 检验项目/Test Items |  |  |  |  |  | 单位 Unit |  | 质量指标/Quality Indicators | 检验结果 Test Results |  |
| 7 | 腐蚀性 (100℃±2℃，120h±2h) Corro-sion | 试验后金属片质量变化 Weight Change of Metal Strips after testing | 锌/Zinc |  |  |  | mg/cm² |  | -0.4 ～ +0.4 | {锌} |  |
|  |  |  | 紫铜/Copper |  |  |  | mg/cm² |  | -0.4 ～ +0.4 | {紫铜} |  |
|  |  |  | 黄铜/Brass |  |  |  | mg/cm² |  | -0.4 ～ +0.4 | {黄铜} |  |
|  |  |  | 铸铁/Cast Iron |  |  |  | mg/cm² |  | -0.2 ～ +0.2 | {铸铁} |  |
|  |  |  | 铝/Aluminum |  |  |  | mg/cm² |  | -0.1 ～ +0.1 | {铝} |  |
|  |  |  | 钢/Steel |  |  |  | mg/cm² |  | -0.2 ～ +0.2 | {钢} |  |
|  |  |  | 镀锡铁皮/Tinned Iron |  |  |  | mg/cm² |  | -0.2 ～ +0.2 | {镀锡铁皮} |  |
|  |  | 试验后试液性能 Fluid Properties after testing | 外观/Appearance |  |  |  | ---------- |  | 无凝胶，在金属表面无粘附物 No gel; no adhering crystals on the metal surface | 无凝胶，在金属表面无粘附物 No gel; no adhering crystals on the metal surface |  |
|  |  |  | pH值/pH |  |  |  | ---------- |  | 7.0 ～ 11.5 | {腐蚀性 pH} |  |
|  |  |  | 沉淀物(体积分数） Sediments ( Volume Fraction ) |  |  |  | % |  | ≤0.10 | {腐蚀性 试液沉淀物} |  |
|  |  | 试验后金属片外观/Appearance of Metal Strips after testing |  |  |  |  | ---------- |  | 无肉眼可见坑蚀和表面粗糙不平，允许脱色或色斑 No visible pitting or roughness; Permitted discoloration or staining. | 无肉眼可见坑蚀和表面粗糙不平，允许脱色或色斑 No visible pitting or roughness; Permitted discoloration or staining |  |
|  |  | 试验后橡胶皮碗状态 Rubber Cups characteristics after testing |  | 硬度降低值/IRHD Hardness Decrease |  |  | ---------- |  | ≤15 | {腐蚀性 硬度降低值} |  |
|  |  |  |  | 根径增值 Increase in Base Diameter |  |  | mm |  | ≤1.4 | {腐蚀性 根茎增值} |  |
|  |  |  |  | 体积增加值 Volume Increase |  |  | % |  | ≤16 | {腐蚀性 体积增加值} |  |
|  |  |  |  | 外观/Appearance |  |  | ---------- |  | 表面不发黏，无炭黑析出 No stickiness on the surface, and no carbon black separation. | 表面不发黏，无炭黑析出 No stickiness on the sur-face, and no carbon black separation. |  |

第3页 共7页

Page 3 of 7

| 续上表/Continued |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 序号 NO. | 检验项目/Test Items |  |  |  |  | 单位 Unit | 质量指标/Quality Indicators | 检验结果 Test Results |
| 8 | 蒸发性能（质量损失） (100℃±2℃，168h±2h) Evaporation (Loss by Mass) |  |  | 蒸发损失 Evaporation Loss |  | % | ≤80 | {蒸发损失} |
|  |  |  |  | 残余物性质 Properties of Residue |  | ------- | 用指尖摩擦时，沉淀中不含有颗粒性砂粒和磨蚀物 No gritty particles or abrasivescontained in the sediment when rubbed between the fingertips. | 用指尖摩擦时，沉淀中不含有颗粒性砂粒和磨蚀物 No gritty particles or abrasivescontained in the sediment when rubbed between the fingertips. |
|  |  |  |  | 残余物倾点 Pour Point of Residue |  | ℃ | ≤-5 | {倾点} |
| 9 | 低温流动性 Low Temperature Fluidity |  | -40℃±2℃ (144h±2h） | 外观 Appearance |  | ------- | 清亮透明均匀 Clear, transparent and homogeneous | 清亮透明均匀 Clear, transparent and homogeneous |
|  |  |  |  | 气泡上浮至液面的时间 Bubble flow time |  | s | ≤10 | {-40气泡上浮的时间} |
|  |  |  |  | 沉淀物 Sediments |  | ------- | 无/None | 无/None |
|  |  |  | -50℃±2℃ (6h±0.2h) | 外观 Appearance |  | ------- | 清亮透明均匀 Clear, transparent and homogeneous | 清亮透明均匀 Clear, transparent and homogeneous |
|  |  |  |  | 气泡上浮至液面的时间 Bubble flow time |  | s | ≤35 | {-50气泡上浮时间} |
|  |  |  |  | 沉淀物 Sediments |  | ------- | 无/None | 无/None |
| 10 | 容水性 (22±2h) Water Tolerance | -40℃±2℃ |  | 外观/Appearance |  | ------- | 清亮透明均匀 Clear, transparent and homogeneous | 清亮透明均匀 Clear, transparent and homogeneous |
|  |  |  |  | 气泡上浮至液面的时间 Bubble flow time |  | s | ≤10 | {容水性气泡上浮时间} |
|  |  |  |  | 沉淀物 Sediments |  | ------- | 无/None | 无/None |
|  |  | 60℃±2℃ |  | 外观 Appearance |  | ------- | 清亮透明均匀 Clear, transparent and homogeneous | 清亮透明均匀 Clear, transparent and homogeneous |
|  |  |  |  | 沉淀量（体积分数） Sediments (Volume Fraction) |  | % | ≤0.05 | {容水性沉淀量} |
| 11 | 抗氧化性 (70℃±2℃） (168h±2h) Resistance to oxidation | 金属片外观/Appearance of Metal Strips |  |  |  | ------- | 无可见坑蚀和点蚀，允许痕量胶质沉积，允许试片脱色 No visible pitting or etching. Trace gum deposit and strip discoloration permitted. | 无可见坑蚀和点蚀，允许痕量胶质沉积，允许试片脱色 No visible pitting or etching. Trace gum deposit and strip discoloration permitted. |
|  |  | 金属片质量变化 Mass Change of Metal Strips |  |  | 铝/Aluminum | mg/cm² | -0.05 ～ +0.05 | {铝 抗氧化} |
|  |  |  |  |  | 铸铁/Cast Iron | mg/cm² | -0.3 ～ +0.3 | {铸铁 抗氧化} |

第4页 共7页

Page 4 of 7

| 续上表/Continued |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 序号 NO. | 检验项目/Test Items |  |  |  |  | 单位 Unit | 质量指标/Quality Indicators | 检验结果 Test Results |
| 12 | 液体稳定性（ERBP变化） Fluid Stability (Change in ERBP) |  | 高温稳定性/High-Temperature Stability (185℃±2℃ 120min±5min） |  |  | ℃ | ±5 | {高温稳定性} |
|  |  |  | 化学稳定性/Chemical Stability |  |  | ℃ | ±5 | {化学稳定性} |
| 13 | 橡胶适应性 (120℃±2℃) (70h±2h） Rubber Compatibility | 丁苯橡胶皮碗 (SBR) SBR Rubber Cups |  | 根径增值 Increase in Base Diameter |  | mm | 0.15 ～ 1.40 | {橡胶根茎增值} |
|  |  |  |  | 硬度降低值/IRHD Hardness Reduction |  | ------- | ≤15 | {橡胶硬度降低值} |
|  |  |  |  | 体积增加值 Volume Increase |  | % | 1 ～ 16 | {橡胶体积增加值} |
|  |  |  |  | 外观 Appearance |  | ------- | 不发黏，无鼓泡，不析出炭黑 No tackiness, no blistering, and no carbon black sloughing. | 不发黏，无鼓泡，不析出炭黑 No tackiness, no blistering, and no carbon black sloughing. |
|  |  | 三元乙丙橡胶试件 (EPDM) EPDM Rubber Test Specimens |  | 硬度降低值/IRHD Hardness Reduction |  | ------- | ≤15 | {橡胶硬度降低值 试件} |
|  |  |  |  | 体积增加值 Volume Increase |  | % | 0 ～ 10 | {橡胶体积增加值 试件} |
|  |  |  |  | 外观 Appearance |  | ------- | 不发黏，无鼓泡，不析出炭黑 No tackiness, no blistering, and no carbon black sloughing. | 不发黏，无鼓泡，不析出炭黑 No tackiness, no blistering, and no carbon black sloughing. |
| 14 | 液体相容性 (22h±2h) Fluid Compatibility | -40℃±2℃ |  |  | 外观 Appearance | ------- | 清亮透明均匀 Clear, transparent and homogeneous | 清亮透明均匀 Clear, transparent and homogeneous |
|  |  |  |  |  | 沉淀 Sediments |  | 无/None | 无/None |
|  |  | 60℃±2℃ |  |  | 外观 Appearance | ------- | 清亮透明均匀 Clear, transparent and homogeneous | 清亮透明均匀 Clear, transparent and homogeneous |
|  |  |  |  |  | 沉淀量(体积分数) Sediments (Volume Fraction) | % | ≤0.05 | {液体相容 沉淀体积} |
| 15 | 水含量(质量分数）/Water Content (Mass Fraction) |  |  |  |  | ω/% | ≤0.2 | {水含量} |
| 16 | 储备碱度/Reserve Alkalinity |  |  |  |  | mL | 实测/Test Results | {储备碱度} |

第5页 共7页

Page 5 of 7

| Attached photo/附件照片 |  |  |
| --- | --- | --- |
| Front View | Back View | Top View |
| Bottom View | Left Side | Right Side |
| Sealing Photo | Liquid Color Photo | Bottle Wall Thickness Photo/瓶壁厚 |

第6页 共7页

Page 6 of 7

| 续上表/Continued |  |  |  |
| --- | --- | --- | --- |
| Attached photo/附件照片 |  |  |  |
| Full Bottle Weight | Empty Bottle Weight |  | Lid Weight |
| Subsidence trend/沉降趋势 |  |  |  |
| VOl% H2O (mL) BF (mL) 3 0.12 3.88 5 0.2 3.8 8 0.32 3.68 12 0.48 3.52 16 0.64 3.36 |  | THF:16mL Total Vol. / Tube：20mL Total Vol. (Brake Fluid + Water) / Tube:4mL VOl%= Volume of water / (Volume of brake fluid + Volume of water) × 100% |  |
| Brake fluid/water mixture (no THF) |  | Brake fluid/water/THF mixture |  |

第6页 共7页

Page 6 of 7

| 续上表/Continued |  |
| --- | --- |
| Sample status after 24 hours | Sample status after three weeks |
| 检验员/Inspector： 审核员/Reviewr： |  |

地址/Addr：福建省泉州市鲤城区江南高新电子技术园紫安路5号 (No. 5 Zi'an Road, Jiangnan High-tech Electronic Technology Park, Licheng District, Quanzhou City, Fujian Province)

电话/Tel:  400-6228-928

E-mail: tgq@chebaoauto.com

- 网址/web: http://www.qzcbzdy.com                                                 检验单位（盖章）

- Testing Organization (Seal)